## Slide 1: Performance Engineered Concrete Mixture Specifications Understanding the Parameters that Influence Critical Performance
Dr Peter Taylor, PE (IL)

## Slide 2: The Challenge
  Contractors want
    Workability
    Uniformity
  Owners want
    Durability
    FOD free
  Everyone wants
    Local materials
    Competitive

## Slide 3: Performance Engineered Mixtures What is it?
A program to
  Understand what makes concrete “good”
  Specify the critical properties and test for them
  Prepare the mixtures to meet those specifications

## Slide 4: What is it?
Performance – choosing what we need
Engineered – delivering what is needed
Mixtures – focus on the mixture, for now

## Slide 5
Extract from a slide used at NC2 in 2008

## Slide 6: The Team
FHWA - Gina Ahlstrom, Mike Praul
Consultants – Tom VanDam, Cecil Jones, Tom Cackler
Researchers – Jason Weiss, Tyler Ley

## Slide 7: Why bother?
Current approaches
  May not measure critical parameters
  Are often built around previous failures – thereby introducing unintended consequences
  Limit innovation
Need to deliver mixtures that meet needs, reliably

## Slide 8: Field Testing
Almost 100 years ago
Today
What has changed?

## Slide 9
But I have been doing it this way for 30 years…

## Slide 10: Why bother?
Iowa Highway Research Board funded project
Collecting data on overlay performance in the whole IA system
This plot represents 12 foot slabs showing Pavement Condition Index (PCI) vs age
Typical of all data collected

## Slide 11: Why bother?
Clear bifurcating data set
  Orange = normal
  Blue = premature distress
    30/257 data points
    Joints
    Foundation system
    Design

## Slide 12: Why bother?
Modelling system performance insists we use all data = gray line
  27 years before 60% Pavement Condition Index
If we could improve our practices to eliminate the premature failure
  45 years before 60% PCI
Adds ~20 years

## Slide 13: Quality

## Slide 14: A Better Specification
  Require the things that matter
    Transport properties (everywhere)
    Aggregate stability (everywhere)
    Strength (everywhere)
    Cold weather resistance (cold locations)
    Shrinkage (dry locations)
    Workability (everywhere)

## Slide 15: Critical Properties
Transport properties (permeability)
  All deterioration mechanisms involve fluid movement
  Keep water out = longer life
  Measurement has been difficult
    Boiled water
    RCPT

## Slide 16: Critical Properties
Aggregate Stability
  If aggregates expand = damage
    Alkali aggregate reaction
    D-Cracking

## Slide 17: Critical Properties
Strength
  Strong enough (But not much more) It comes along for the ride
  Beware of shrinkage, high heat

## Slide 18: Critical Properties
Cold Weather
  Freeze-thaw
    Entrained air
  De-icing salts
    Sufficient SCM

## Slide 19: Salts can cause chemical attack
Calcium oxychloride is formed
  Calcium from cement
  Chlorides from salts
  Expands 31%
  At 40°F
Sutter
CaCl2 @ 40°F
Notes: There are signs of chemical attack in some cases. The oxychloride later decomposes and disappears. This from Larry Sutter’s work for SD. Have to have the right temperature.

## Slide 20: Salts can cause chemical attack
Calcium oxychloride
MgCl2 @ 40°F
Notes: There are signs of chemical attack in some cases. The oxychloride later decomposes and disappears. This from Larry Sutter’s work for SD. Have to have the right temperature.

## Slide 21: Critical Properties
Shrinkage
  Random cracking
  Warping

## Slide 22: Critical Properties
Workability
  Not too wet
  Not too dry

## Slide 23: A Better Specification
  Measure the right things at the right time
    Prequalification
    Process control
    Acceptance

## Slide 24: A Better Specification
  A buffet of approaches
    Prescriptive: w/cm, paste volume
    Performance: Formation factor

## Slide 25: A Better Specification
  AASHTO PP84 published in March
    Guide Specification
    “Deemed to satisfy”
    Avoids bonus discussion – that is local
    Provisional = meaning we can modify as we learn things

## Slide 26: Transport Properties/Permeability (6.6)

## Slide 27: Aggregate Stability (6.7)

## Slide 28: Concrete Strength (6.3)

## Slide 29: Hardened Cement Paste Freeze-Thaw Durability (6.5)

## Slide 30: Reducing Unwanted Cracking Due to Shrinkage (6.4)

## Slide 31: Workability (6.8)

## Slide 32
Time for a break

## Slide 33: Quality

## Slide 34: Acceptance Testing
Should be
  Fast
  Reliable
  Meaningful
  Affordable

## Slide 35: Test Methods
Tests for those critical properties
    VKelly
    Box
    Resistivity / Formation factor
    Bucket / Sorptivity
    Dual ring
    SAM

## Slide 36: VKelly
Kelly ball test
  Developed in the 1950s in US
  Standardized in California DOT test
  Comparable to slump test

## Slide 37: VKelly
Measure initial slump (initial penetration)
Start vibrator for 36 seconds at 8000 vpm
Record depth every 6 seconds
Repeat
Plot on root time
Calculate slope = VKelly Index

## Slide 38: Box Test
A test that examines:
  Response to vibration
  Filling ability of the grout (avoid internal voids)
  Ability of the concrete to hold an edge
Ley

## Slide 39: Box Test
The edges of the box are then removed and inspected for honey combing and edge slump
Ley

## Slide 40: Super Air Meter
Reports air content and SAM number
SAM number correlates well with freeze thaw testing
Ley

## Slide 41: Cold Weather Resistance
Freeze Thaw (Time to Saturation)
Weiss

## Slide 42: Cold Weather Resistance
Resistance to Salts
  Expansive calcium oxychloride formation
    From MgCl2 and CaCl2
  Measure with – Low temperature differential scanning calorimetry (LT-DSC)
Sutter

## Slide 43: Formation Factor
Resistivity
  Then calculate Formation Factor based on
    Moisture
    Temperature
    Geometry
    Curing conditions
    Ionic concentration of the pore solution
    F = Resistivity (bulk) Resistivity (solution)
Weiss

## Slide 44: Shrinkage
Cracking risk
Warping

## Slide 45: Ring Test
Assesses cracking risk
Starts immediately

## Slide 46: Dual Ring Test
Plan View
Concrete
Invar ring
Strain gauge
This ring can measure both expansion and contraction.
As the concrete shrinks the ring can measure the strains that occur.
We force a temperature gradient in the concrete and make it crack and compare that to 60% of the split tension capacity after 7 days.
Weiss

## Slide 47: Quality

## Slide 48: Construction
QC should include
  Unit weight
  Calorimetry
  Maturity
  Strength development
  Air void stability
  And a response…
Risk management

## Slide 49: Uniformity
Deliver the same mixture in every truck

## Slide 50: Foam Drainage
Air void systems can change with working / pumping
Depends on system chemistry

## Slide 51: Calorimetry
  Calorimetry tells us about the chemistry of the system (Uniformity)

## Slide 52: Unit weight
Uniformity
  Affected by air and water

## Slide 53: Maturity
Maturity readings
  Sensors in the pavement determine in-place maturity and thereby strength for opening
Notes: the maturity of the pavement from data loggers instrumented in the field on 9/22 and 9/24. From this figure it can be seen that, for the specific site conditions on 9/22 and 9/24, the pavement reached a 5800 ºChrs maturity value (equivalent to a flexural strength of 550psi) in 152 hours (6.3 Days). So using the concept of maturity, the pavement can be opened to construction traffic at least 3 days in advance of the current minimum opening requirement of 10 days. This is because the strength gain of the pavement is faster than the beams due to the greater mass of concrete (higher heat of hydration) and greater exposure to the environment (The environment could increase or decrease the strength gain compared to lab cured specimens depending on the temperature and moisture conditions). It measures the actual in place pavement under actual field conditions. Test specimens cured at standard conditions represent the concrete strength under laboratory conditions which are different than what the pavement experiences. So the concept of maturity can be used to open pavements for construction traffic sooner, which in turn can help reduce costs, speed up the construction operations and also helps in safety related issues.
Maturity meters currently available in the market automate the process shown in these figures. They are very easy to use and relatively inexpensive. By using the maturity concept to open pavements to traffic sooner, CALTRANs can benefit significantly in terms of time and money savings.

## Slide 54: Quality

## Slide 55: Better Mixtures
History
  Structural concrete 1:2:4
  Other concrete 1:3:6
  Waterproof concrete Add salt
  No chemicals
  No SCMs
  Precision was ugly
  Bulking made it worse

## Slide 56: Proportioning Approaches Present
ACI 211
  Last revised in 1991
  Linear
Developed
  Before water reducers
  Before supplementary cementitious materials
Primarily focused on structural concrete
  100 mm (4”) slump
  30 MPa (~4000 psi)

## Slide 57: Workability

## Slide 58: Workability

## Slide 59: Preconceptions
More cement = more strength
Strength is everything
Slump indicates quality
Gradations of individual fractions are critical

## Slide 60: Proposed Mixture Proportioning Procedure
Koehler
Aggregate system
Paste Quality
Paste Quantity

## Slide 61: How do we proportion to achieve design goals?
Notes: This chart indicates which of the three mixture parameters affects what critical property. The yellow stripe is where the specification should reside. All else should be left to the contractor to match available materials with their equipment while still meeting spec requirements.

## Slide 62: Doing the Sums
  The wonders of a spreadsheet and a solver function…
Measure Va

## Slide 63: Does it Work?
West Des Moines spec
    5% minimum air behind the paver
    0.42 w/cm target
    35% fly ash
    Cracking risk
      MN recommended 400 pcy cement
      Blankets

## Slide 64: What do we get?
Concrete that delivers what is needed
  Efficiently w.r.t.
    Cost
    Environmental impact
  Reliably
  More riding, less waiting

## Slide 65: What next?
Understanding and education
Validate tests in the field
Parallel testing
New tests
Pooled fund to pay for it

## Slide 66: Implementation

## Slide 67: Implementation

## Slide 68: Closing
The framework is in place
The details need work